XOANONS® Reactive silicone leveling agent

| Model number |  |  | Incorporation |  |
| --- | --- | --- | --- | --- |
| XOANONS®WE-D7220 |  |  | Easy to add with pre-diluted solvent the same as that in the coating system. Can added as post-addition. |  |
| Specification |  |  | Suggest addition |  |
| Composition | Silicone polyether acrylate with crosslinked free radical |  | Addition to total formulation 0.1-1.0% |  |
| Appearance | Light to dark green clear liquid |  | Storage stability |  |
| Solvent | —— |  |  |  |
| Density | 1.03-1.07g/ml(25±1)℃ |  | Keep intact 24 months in original package.Products |  |
| Viscosity | 500-2500 mPa·s |  | beyond the storage period may continue to be used after |  |
|  | (Rotating viscometer)(25±0.2)℃ |  | inspection. The container must be closed immediately |  |
| Active substance | 100% |  | after use. |  |
| Flash point | ＞100℃ |  |  |  |
| Note: This datasheet is intended to give typical results, not standard. |  |  |  |  |
| Subject to COA. |  |  | Applicate recommendation |  |
|  |  |  | Mobility | 4 |
| Application system |  |  | Slip | 4 |
|  |  |  | Stick resistance | 2 |
| UV Cure |  |  | Substance wetting | 4 |
|  |  |  | Defoaming | 0 |
| Properties |  |  | 0=unavailable 5=very effective |  |
| - Radiation reactive silicon additive. Improve mechanical properties and reduce friction, excellent ability of defoaming. |  |  |  |  |
| - Improve leveling. |  |  |  |  |
| - Good compatibility in varnish. |  |  | Package |  |
|  |  |  | 25KG / 180KG |  |