XOANONS® Dispersing agent

| Model number |  |  |  |  |
| --- | --- | --- | --- | --- |
| XOANONS®WE-D200R |  |  |  |  |
| Specification |  |  |  |  |
| Composition | Low molecular weight unsaturated fatty acid polyamide polyester solution |  |  |  |
| Appearance | Yellow to brownish yellow clear liquid |  |  |  |
| Solvent | DPMA |  |  |  |
| Active substance | 50% |  |  |  |
| Density | 1.00-1.04g/ml(25±1)℃ |  |  |  |
| Viscosity | 10-80s(Tu-4 viscometer)(25±0.2)℃ |  |  |  |
| Flash point | ≥70℃ |  |  |  |
| Note: This datasheet is intended to give typical results, not |  |  |  |  |
| standard.Subject to COA. |  |  |  |  |
| Application system |  |  |  |  |
| Solvent-based |  |  |  |  |
| Properties |  |  |  |  |
| - Excellent dispersing efficiency and viscosity reduction effect. |  |  |  |  |
| - High gloss. Increase color intensity. |  |  |  |  |
| - Increase transparency and shading. |  |  |  |  |
| - It is very suitable for the preparation of organic bentonite slurry. |  |  |  |  |
| - In particular, it is recommended for use in architectural, industrial and anticorrosive coating system. |  |  |  |  |

| Incorporation |  |  |
| --- | --- | --- |
| Should be incorporated to the mill base before pigments adding. |  |  |
| Suggest addition |  |  |
| Inorganic pigment |  | 1-2% |
| Organic pigment |  | 1-5% |
| TiO2 |  | 0.5-1.0% |
| Bentonite |  | 30-50% |
| Storage stability |  |  |
| Stir well before use. Stratification or turbidity may occur at low temperature. Heated to 30-60℃ and fully mixed without side effect to use. Keep intact 24 months in original package.Products beyond the storage period may continue to be used after inspection. The container must be closed immediately after use. |  |  |
| package |  |  |
| 25KG / 180KG |  |  |